## Slide 1: Training clusters

## Slide 2: Data in clusters: filter outliers
We take the mean integrated intensity for each spectrum in cluster
   filter outliers
Just use trimmed mean & trim cluster? (i.e. discard equal number of top and bottom values):
  CI = round( (0.05 * n_cluster)/2 )
  Cluster = cluster[CI:-CI]
Use mean shift outlier model to determine outliers? (Check influence of each value on mean cluster, discard ones with most influence, i.e. not equal number top and bottom)

## Slide 3: Finding dE1 -- Laurien

## Slide 4: Finding dE1
Note: not 1!

## Slide 5: Values
﻿dE1 cluster 0 avg: 1.072 , std: 0.1827 , min: 0.615
dE1 cluster 1 avg: 0.9167 , std: 0.1337 , min: 0.585
dE1 cluster 2 avg: 0.8621 , std: 0.1302 , min: 0.54
dE1 cluster 3 avg: 0.8554 , std: 0.1337 , min: 0.525
dE1 cluster 4 avg: 0.8188 , std: 0.1224 , min: 0.51
Thicker sample  lower dE1:
  Makes sense: thicker sample  higher overall influence  sooner visable

## Slide 6: How to determine dE1?
Lowest of all spectra?
Lowest of cluster averages?
Point where cluster derivative average crosses 0?

## Slide 7: Finding dE2 -- Laurien

## Slide 8: Finding dE2

## Slide 9: Mean intensity and sigma of bins

## Slide 10: Zoom in on end

## Slide 11: Why not converging to 1?
Values of all spectra at single energy

## Slide 12: Finding dE2

## Slide 13: Why the spikes? all vacuum values at 12.09eV

## Slide 14: Why the spikes?
Sonia????

## Slide 15: Solutions
Spikes should be filterable (some comparison to neighbours)
Value not converting to one more difficult I think:
  Take higher threshold?
  Assume ZLP indeed still has influence and set higher dE2?

## Slide 16: PS: log helps for the spikes, not for the convergence

## Slide 17: For log: how to handle negatives (and 0)?
Problem:
For vacuum cluster:
  Ratio negative/pos: ﻿2.5E5/1.86E7 = 0.013
  Avg negative: ﻿-39
  Min negative: -770
  Avg positive: ﻿16900
Solution?
I = I – min(I)
  Per spectrum?
  Per cluster?
I[I<1] = 1 ?

## Slide 19: BTW: Lau only trained -0.5eV to 20eV
I figured I’d just take the range of the sample?